#### TECHNICAL DATA SHEET

#### POLARFOAM™ PF-7217-0

## ZERO ODP CLASS 1 SPRAY APPLIED RIGID

### POLYURETHANE FOAM THERMAL INSULATION

Polarfoam™ PF-7217-0 is a two component spray-applied rigid polyurethane foam system specially formulated to meet the zero ozone depletion potential (ODP) requirement of the Montreal Protocol and to meet the Classification 1 requirement of the ASTM E-84.

This friendly 0 ODP environmental foam product is also manufactured with recycled plastics and renewable soya beans material.

## PHYSICAL PROPERTIES

| Method | Description | Value |
| --- | --- | --- |
| ASTM D1622 | Density | 35 +/- 2 Kg/m³ (2.2 +/- 0.1 lb/ft³) |
| ASTM C518 | Thermal Resistivity 2 days @ 23°C -0°C (32°F)/25°C (77°F) -10°C (50°F)/35°C (95°F) | 1.26 m².°C/W (7.14 ft².h.°F/BTU.in) 1.19 m².°C/W (6.74 ft².h.°F/BTU.in) |
| ASTM D2856 | Closed Cell Content (%) | >92 |
| ASTM D1621 | Compressive Strength (parallel) | 152 kPa (22 psi) |
| ASTM D2126 | Dimensional Stability (% Volume Change) 80°C, ambient R.H. 70°C, 97% R.H. -30°C, ambient RH | 7 days -0.1 +3.6 -1.3 |
| ASTM D2842 | Water Absorption (% Volume) (96 hrs. immersion) | 1.0 |
| ASTM E84 | Surface Burning Characteristics, thickness Flame spread index Smoke developed | 2” 3” 15 25 400 450 |

The information herein is to assist customers in determining whether our products are suitable for their applications.  We request that customers inspect and test our products before use and satisfy themselves as to contents and suitability.  Nothing herein shall constitute a warranty, express or implied, including any warranty of merchantability or fitness, nor is protection from any law or patent inferred.  All patent rights are reserved.  The foam product is combustible and must be covered by an approved thermal barrier.  The exclusive remedy for all proven claims is replacement of our materials.

POLARFOAM™  PF-7217-0

# LIQUID COMPONENTS PROPERTIES

## PROPERTY			ISOCYANATE			RESIN

Colour				Brown					Brownish

Viscosity @ 25°C		150-250 cps				150-350 cps

Specific gravity		1.20-1.24				1.20-1.24

Shelf life*			12 months				6 months

Mixing ratio (volume)		100					100

Vapour pressure @ 25°C	10-7 psi					7 psi

*See MSDS for more information.

# FOAM PROCESSING PARAMETERS

Type of machine:			Gusmer H20/35, #62 mix chamber

Components Iso&Res. temperature	40°C (105°F)

Components Iso&Res. temperature:	5860-6900 kPa (850-1000 psi)

Ambient temperature:			20°C (68°F)

Thickness per pass:			35mm (1 ¼ inch)

Number of passes:			2

Substrate:				Plasterboard

# REACTIVITY PROFILE

Cream time		Gel time		Tack free time		End of rise

0-1 sec.		2 sec.			4 sec.			3 sec.

# RECOMMENDED PROCESSING CONDITIONS

Mixing Ratio Iso&Res:		1/1

Mixing temperature:			40°C (105°F)

Mixing pressure (minimum):		5516 Kpa (800 psi)

Substrate & Ambient temperature:	>10°C (50°F)

Maximum thickness per pass:		2 inches

Note:  Never apply foam with pass thickness greater than 2 inches because foam will be dimensionally unstable (too much of elongated cells).

General Information:

It is recommended that the foam be covered with an approved thermal barrier in accordance to the local and national building codes when used in buildings and a protective coating when used outside.  This product should not be used when the continuous service temperature of the substrate is outside the range of –60°C to 82°C.

April 6, 2006